# MATERIAL SELECTION GUIDE

We, TAF., hereby reproduce the following summary of corrosion resistance of  various   special  materials. It must be understood that these data are shown to serve only as a general suggestion and not as a guarantee.  Final selection must be based on actual evaluation of the metal in the corrosive medium under study.

| A - Fully Resistant. ( - Subject to pitting at air line or when allowed to dry B - Slightly Attacked ( - May attack when sulfuric acid is present. C - Unsatisfactory |
| --- |
| CORROSION DATA -SALTS | Hastelloy “B” | Hastelloy “C” | Carpenter 20 | Monel | Inconel | Stainless Steel 316 | Tantalum | Titanium | Zirconium |
| Media | Concentration | Temperature oF |  |  |  |  |  |  |  |  |  |
| Acetyl Chloride |  | Cold & Boiling |  |  | B | AB |  | B |  |  |  |
| Aluminum Acetate | Saturated |  | A | A | A | AB | AB | A | A |  |  |
| Aluminum Chloride | 5% | Room | A | A | A | AB |  | C | A | A | A |
| Aluminum Fluoride | 5% | Room | A | A | A | AB |  | B | C |  |  |
| Aluminum Hydroxide | Saturated |  |  |  | A | AB |  | A | A |  |  |
| Aluminum Oxalate |  |  | A | A | A | AB |  |  |  |  |  |
| Aluminum Potassium Sulfate | 2% | Room |  |  | A | AB |  | A | A |  |  |
| Aluminum Potassium Sulfate | 10% | Room |  | A | A | AB |  | A | A |  |  |
| Aluminium Potassium |  |  |  |  |  |  |  |  |  |  |  |
| Sulfate | 10% | Boiling |  |  | A | C |  | A | A |  |  |
| Aluminium Potassium Sulfate | Saturated | Boiling |  |  | A | C |  | B | A |  |  |
| Aluminium Sulfate | 10% | Room | A | A | A | AB |  | A | A |  | A |
| Aluminium Sulfate | 10% | Boiling | A | A | A | C |  | A | A |  | A |
| Aluminium Sulfate | Saturated | Room | A | A | A | AB |  | A | A |  |  |
| Aluminium Sulfate | Saturated | Boiling |  |  | A | C |  | A | A |  |  |
| Ammonia |  |  |  |  |  |  |  |  |  |  |  |
| (Anhydrous Dry) |  |  | A | A | A | AB | A | A |  |  |  |
| Ammonium Alum |  |  | A | A | A |  | AB | A | A |  |  |
| Ammonium Alum (Slightly Ammoniacal) |  |  | A | A | A |  | AB | A | A |  |  |
| Ammonium Bicarbonate |  | Hot |  |  | A | AB | A | A | A |  |  |
| Ammonium Bromide | 5% | Room | A | A | A | AB |  | A | A |  |  |
| Ammonium Carbonate | All conc. | Hot & Cold | A | A | A | A | A | A | A |  |  |
| Ammonium Chloride | 1% | Room | A | A | A | A |  | A | A | A | A |
| Ammonium Chloride | 10% | Boiling | A | A | A | AB |  | (A | A | A | A |
| Ammonium Chloride | 28% | Boiling | A | A | A | AB |  | (A | A |  | A |
| Ammonium Chloride | 50% | Boiling |  | A | A | AB |  | (A | A |  | A |
| Ammonium Hydroxide |  |  | A | A | A | C | A | A |  | A | A |
| Ammonium Monosulfate |  |  | A | A | A | AB |  | A | A |  |  |
| Ammonium Nitrate | 5% | Room | C | A | A |  | AB | A | A |  |  |

| CORROSION DATA - SALTS (continued) | Hastelloy "B" | Hastelloy "C" | Carpenter 20 | Monel | Inconel | Stainless Steel 316 | Tantalum | Titanium | Zirconium |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Media | Concentration | Temperature 0F |  |  |  |  |  |  |  |  |  |
| Ammonium Oxalate | 5% | Room | A | A | A | AB | AB | A | A |  |  |
| Ammonium Persulfate | 5% | Room | C | A | A | C | AB | A | A |  |  |
| Ammonium Phosphate | 5% | Room | A | A | A | AB | AB | A | A |  |  |
| Ammonium Sulfate | 1% to 5% Agitated, Aerated | Room | A | A | A | AB |  | A | A |  | A |
| Ammonium Sulfate | 10% | Boiling | A | B | A | AB |  | (A | A |  |  |
| Ammonium Sulfate | Saturated | Boiling | A | B | A | AB |  | (A | A |  |  |
| Ammonium Sulfite | Saturated | Cold & Boiling |  |  | A | C | C | A | A |  |  |
| Amyl Acetate |  |  | A | A | A | AB | AB |  | A |  |  |
| Amyl Chloride |  |  | A | A | A |  |  |  | A |  |  |
| Aniline Hydrochloride | 5% | Room | A | A |  |  |  | C | A |  | A |
| Antimony Trichloride |  | Room |  |  |  | AB |  | C | A |  |  |
| Barium Carbonate |  | Room | A | A | A | AB |  | A | A |  |  |
| Barium Chloride | 5% to Sat. | Room | A | A | A | AB |  | A | A | A | A |
| Barium Chloride | Aqueous Sol. | Hot |  |  | A | AB |  | (A | A |  | A |
| Barium Hydrate |  |  | A | A | A | AB | AB | A |  |  |  |
| Barium Nitrate | Aqueous Sol. | Hot |  |  | A |  | AB | A | A |  |  |
| Barium Sulfate |  | Room |  |  | A | AB |  | A | A |  |  |
| Butyl Acetate |  |  | A | A | A | AB |  |  | A |  |  |
| Calcium Carbonate |  | Room | A | A | A | A | A | A | A |  |  |
| Calcium Chlorate | Dilute | Hot or Cold |  | A | A | AB | AB | A | A |  |  |
| Calcium Chloride | Dil. Or Conc. | Room | A | A | (A | AB | AB | (A | A | A | A |
| Calcium Hydroxide | 10% to 20% | Boiling | A | A | A | A | A | A | A |  |  |
| Calcium Hydroxide | 50% | Boiling | A | A | A | A | A | B |  |  |  |
| Calcium Hypochlorite | 2% | Room | C | A | C | C | C | (A |  | A | B |
| Calcium Sulfate | Saturated | Room |  |  | A | AB |  | A | A |  |  |
| Carbon Bisulfide |  | Room |  |  | A | AB | AB | A | A |  |  |
| Carbon Tetrachloride | Pure | Room | A | A | A | A | A | A | A | A | A |
| Carbon Tetrachloride | 5% to 10% Aqueous Sol. | Room | A | A | A | A |  | B |  | A | A |
| Chlorebenzene (Pure) | Concentrated | Room |  |  | B | A |  | A |  |  |  |
| Copper Acetate | Saturated | Room | A | A | A |  | AB | A | A |  |  |
| Copper Carbonate | Sat. Sol |  | A | A | A |  | AB | A | A |  |  |
| Copper Chloride | 1% Agitated & Aerated | Room | A | A |  | C | C | (A | A |  |  |
| Copper Chloride | 5% Agitated | Room | A | A |  | C | C | (B | A |  |  |
| Copper Chloride | 5% Aerated | Room | A | A |  | C | C | (C | A |  |  |
| Copper Cyanide | Saturated | Boiling | A | A | B | C | C | A | A |  |  |
| Copper Nitrate | 1% to 5% | Room | C | A | A | C | B | A | A |  |  |
| Copper Nitrate | 50% Aqueous | Room | C | A | A | C | C | A | A |  |  |
| Copper Sulfate | 5% | Room | A | A | A | B | B | A | A | A |  |

| CORROSION DATA - SALTS (continued) | Hastelloy "B" | Hastelloy "C" | Carpenter 20 | Monel | Inconel | Stainless Steel 316 | Tantalum | Titanium | Zirconium |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Media | Concentration | Temperature 0F |  |  |  |  |  |  |  |  |  |
| Cupric Chloride |  | 105 0 | C | A | C | C | C | C | A | A | C |
| Cupric Nitrate |  |  | C | A | A | C | C | A | A |  |  |
| Ethyl Acetate |  |  | A | A | A | A | A |  | A |  |  |
| Ethyl Chloride | 5% | Room | A | A | A | AB |  | A | A |  |  |
| Ethylene Chloride |  | Room |  |  | A | AB |  | A | A |  | AB |
| Ferric Chloride | 5% Still | Room | C | A | C | C | C | C | A | A | C |
| Ferric Chloride | 5% Agitated | Room | C | A | C |  |  | C | A | A | C |
| Ferric Chloride | 5% Aerated | Room | C | A | C | C | C | C | A | A | C |
| Ferric Hydroxide |  | Room | C | A | A | AB | A | A | A |  |  |
| Ferric Nitrate | 1% to 5% | Room | C | A | A | C | C | A | A |  |  |
| Ferric Sulfate | 1% to 5% | Room | C | A | A | C | C | A | A |  |  |
| Ferrous Chloride |  | Room | A | A | C | C | C |  | A |  |  |
| Ferrous Sulfate | Dilute | Room | A | A | A | C | C | A | A |  |  |
| Ferrous Ammonium Citrate |  |  |  |  |  |  |  |  |  |  |  |
| Hydrogen Peroxide |  | Room | B | A | A | AB | AB | (A | A | A | A |
| Hydrogen Peroxide |  | Boiling | B | A | A |  |  | (A | A | A |  |
| Hydrogen Sulfide | Dry | Room | B | A | A | AB | AB | A | A | A |  |
| Hyposulfite Soda (Hypo) |  |  |  |  |  | AB | AB | A | A |  |  |
| Lactic Acid Salts |  |  | A | A | A | AB | AB | A | A |  |  |
| Lead Acetate |  |  | A | A | A | AB |  | A | A |  |  |
| Manganese Carbonate |  |  |  |  | A | AB | AB | A | A |  |  |
| Manganese Chloride | 10% to 50% Aqueous Sol. | Boiling |  |  | B | AB | AB | A | A | A |  |
| Magnesium Carbonate |  |  | A | A | A | AB | AB | A | A |  |  |
| Magnesium Chloride | 1% to 5% Still | Room | A | A | A | AB | AB | A | A | A | A |
| Magnesium Chloride | 1% to 5% Still | Hot | A | A | A | AB | AB | (B | A | A | A |
| Magnesium Hydroxide | Thick Suspension | Room | A | A | A | A | A | A | A |  |  |
| Magnesium Nitrate |  |  | C | A | A |  | AB | A | A |  |  |
| Magnesium Sulphate | 5% | Hot | A | A | A | A | A | A | A |  |  |
| Methylene Chloride | 40% | Room to Boiling | A | A | A | AB |  | A |  |  |  |
| Mercuric Bichloride | 0.07% | Room | C | C |  |  |  | (A | A |  |  |
| Mercuric Chloride | Dilute | Room | C | A | C | AB | AB | C | A | A | A |
| Mercuric Cyanide |  |  | C | A | A |  | AB | A | A |  |  |
| Mercurous Nitrate |  |  | C | A | A |  |  | A | A |  |  |
| Nickel Chloride |  | Room | C | A | A | AB |  | (A | A | A | AB |
| Nickel Nitrate | 10% | Room | AB | A | A | C | C | A | A |  |  |
| Nickel Sulfate | 10% | Room | A | A | A | AB | AB | A | A |  |  |
| Nitrous Oxide | Dry |  | C | A | A | C | C |  | A |  |  |
| Phosphoric Anhydride | Dry | Room |  |  | A |  |  | A | A |  |  |
| Phosphorous Trichloride |  |  | C | A | A |  |  | A | A |  |  |
| Potassium Bichromate | Neutral | Room | C | A | A |  | AB | A | A |  |  |
| Potassium Bromide | 5% | Room | A | A | A | AB |  | (A | A |  |  |
| Potassium Carbonate | 1% | Room | A | A | A | AB | AB | A | A |  |  |

| CORROSION DATA - SALTS (continued) | Hastelloy "B" | Hastelloy "C" | Carpenter 20 | Monel | Inconel | Stainless Steel 316 | Tantalum | Titanium | Zirconium |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Media | Concentration | Temperature 0F |  |  |  |  |  |  |  |  |  |
| Potassium Chlorate |  |  | C | A | A | AB | AB | A | A |  |  |
| Potassium Chloride | 1% to 5% | Room | A | A | A | AB |  | (A | A | A |  |
| Potassium Chloride | 1% to 5% | Boiling | C | A | A | AB |  | (A | A |  |  |
| Potassium Cyanide |  |  | A | A | A | AB |  | A | A |  |  |
| Potassium Dichromate | Neutral |  | C | A | A |  | AB | A | A |  |  |
| Potassium Ferri cyanide | 5% | Room | A | A | A | AB |  | A | A |  |  |
| Potassium Ferro cyanide | 5% | Room | A | A | A | A | A | A | A |  |  |
| Potassium Hydrate |  |  | A | A | A | A | A | A |  |  |  |
| Potassium Hydroxide | 5% | Room | A | A | A | A | A | A | A |  | A |
| Potassium Hydroxide | 27% | Boiling | A | A | A | A | A | A | C |  | A |
| Potassium Hydroxide | 50% | Boiling | A | A | A | A | A | A | C |  |  |
| Potassium Hypochlorite |  |  | C | A | A | C | C | C |  |  |  |
| Potassium Iodide |  |  | A | A | A | AB |  | A | A |  |  |
| Potassium Nitrate | 5% | Room | C | A | A | AB |  | A | A |  |  |
| Potassium Oxalate |  |  | A | A | A |  |  | A | A |  |  |
| Potassium Permanganate | Neutral |  | C | A | A | AB | AB | A | A |  |  |
| Potassium Sulfate | 1% to 5% | Room | A | A | A | AB |  | A | A |  |  |
| Potassium Sulfate | 1% to 5% | Hot |  |  | A | AB |  | A | A |  |  |
| Potassium Sulfide (Salt) |  |  |  |  | A |  |  | A | A |  |  |
| Quinine Bisulfate (Dry) |  |  | A | A | A | AB |  | A | A |  |  |
| Quinine Sulfate (Dry) |  |  | A | A | A | AB |  | A | A |  |  |
| Silver Bromide |  |  | A | A | A | AB |  | (A | A |  |  |
| Silver Chloride |  |  | C | A | A |  |  | C | A |  |  |
| Silver Cyanide |  |  | A | A | A | AB |  | A | A |  |  |
| Silver Nitrate |  |  | AB | AB | A |  | AB | A | A |  |  |
| Sodium Acetate (Moist) | 5% | Room | A | A | A | AB |  | A | A |  |  |
| Sodium Benzoate |  |  | A | A |  | AB |  |  | A |  |  |
| Sodium Bicarbonate | All Conc. | 150O | A | A | A | A | A | A | A |  |  |
| Sodium Bichromate | Neutral |  | C | A | A |  | AB | A | A |  |  |
| Sodium Bisulfate |  |  | A | A | A | AB |  | A | A |  |  |
| Sodium Borate |  |  | A | A | A | AB |  | A | A |  |  |
| Sodium Bromide | 5% | Room | A | A | A | AB |  | A | A |  |  |
| Sodium Carbonate | All Conc. | Room | A | A | A | A | A | A | A | A |  |
| Sodium Chlorate | 25% |  | C | A | A |  | AB | A | A | A |  |
| Sodium Chloride | 5% Still | Room to 150 0 | A | A | A | A |  | (A | A | A | A |
| Sodium Chloride | 20% Aerated | Room | A | A | A | A |  | (A | A | A |  |
| Sodium Chloride | Saturated | Room | A | A | A | A |  | (A | A | A |  |
| Sodium Chloride | Saturated | Boiling | A | A | A | A |  | (A | A | A |  |
| Sodium Citrate |  |  | A | A | A |  | AB | A | A |  |  |
| Sodium Ferricyanide |  |  | A | A | A | AB | AB | (A | A |  |  |
| Sodium Ferrocyanide |  |  |  |  |  |  |  |  | A |  |  |
| Sodium Fluoride | 5% | Room | A | A |  | AB |  | B | C |  |  |

| CORROSION DATA - SALTS (continued) | Hastelloy "B" | Hastelloy "C" | Carpenter 20 | Monel | Inconel | Stainless Steel 316 | Tantalum | Titanium | Zirconium |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Media | Concentration | Temperature 0F |  |  |  |  |  |  |  |  |  |
| Sodium Hydrosulfite |  |  | B | A | A | AB | AB |  | A |  |  |
| Sodium Hydroxide | 10% | Room | A. | A | A | A | A | A | C | B | A |
| Sodium Hypochlorite | 5% | Room | C | A | B | C | C | (A |  | B | B |
| Sodium Hyposulfite | Dilute | Room | A | A | A | AB | AB | A | A |  |  |
| Sodium Lactate |  |  | A | A | A | AB |  | A | A |  |  |
| Sodium Nitrate | All Conc. | Room | C | A | A | AB | AB | A | A | A |  |
| Sodium Nitrite |  |  |  |  |  |  |  | A | A |  |  |
| Sodium Peroxide |  | 212O | C | A | A | AB | AB | A | C |  |  |
| Sodium Phosphate | 5% | Room | A | A | A | AB |  | A | A | A |  |
| Sodium Silicate |  |  | A | A | A | AB |  | A | A |  |  |
| Sodium Sulfate | 5% Still | Room | A | A | A | AB | AB | A | A |  |  |
| Sodium Sulfate | Concentrated | Room | A | A | A | AB |  | A | A |  |  |
| Sodium Sulfide | Saturated | Room | A | A | A |  | AB | A | A | A |  |
| Sodium Sulfite | 5% | Room | C | A | A | B |  | A | A |  |  |
| Stannic Chloride | 5% | Room | A | A | A | C | C | C | A | A | A |
| Stannous Chloride | 5% | Room | A | A | A | AB | AB | B | A |  |  |
| Sulfur Chloride | Dry |  | A | A | A | AB |  | C | A |  |  |
| Sulfur Dioxide | Dry | Room | C | A | A | A | A | A | A | A |  |
| Sulfur Dioxide | Moist | Room | C | A | A | C | C | A | A | A |  |
| Titanium Tetrachloride |  |  | C | A | A | AB |  |  | A |  |  |
| Zinc Chloride | 5% Still | Room | A | A | A | AB |  | B | A | A | A |
| Zinc Chloride | 5% Still | Boiling | AB | AB | A | AB |  | (B | A | A | A |
| Zinc Sulfate | 5% | Room | A | A | A | AB | AB | A | A |  |  |
| Zinc Sulfate | Saturated | Room | A | A | A | AB |  | A | A |  |  |
| Zinc Sulfate | 25% | Boiling | A | A | A | AB |  | A | A |  |  |

| CORROSION DATA - ACIDS | Hastelloy "B" | Hastelloy "C" | Carpenter 20 | Monel | Inconel | Stainless Steel 316 | Tantalum | Titanium | Zirconium |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Media | Concentration | Temperature 0F |  |  |  |  |  |  |  |  |  |
| Acetic Acid | 5% Unaerated | Room | A | A | A | AB | AB | A | A | A | A |
| Acetic Acid | 20% Unaerated | Room | A | A | A | AB | AB | A | A | A | A |
| Acetic Acid | 50% Unaerated | Room | A | A | A | AB | AB | A | A | A | A |
| Acetic Acid | 50% Unaerated | Boiling | A | A | A | AB |  | B | A | A | A |
| Acetic Acid | 100% Unaerated | Room | A | A | A | AB | AB | A | A | A | A |
| Acetic Acid | 100% Unaerated | Boiling | A | A | A | AB | C | B | A | A | A |
| Acetic Anhydride | Unaerated | Room | A | A | A |  | AB | A |  | A | A |
| Acetic Anhydride | Unaerated | Boiling | A | A | A | B | B | A |  | A | A |
| Acetic Vapors | 100% Unaerated | Hot | A | A | A | AB | AB | C |  |  |  |
| Arsenic Acid | 90% | 225 0 |  |  |  |  | B | B |  |  |  |
| Benzoic Acid | 5% | Room | A | A | A | AB | AB | A | A |  |  |
| Boric Acid | 5% | Boiling | A | A | A | AB |  | A | A |  |  |
| Butyric Acid | 5% | Room | A | A | A |  | AB | A | A |  |  |
| Carbonic Acid |  |  | A | A | A | AB | AB | A | A |  |  |
| Carbolic Acid, C.P. |  | Room | A | A | A |  |  | (A | A |  | A |
| Chloroacetic Acid |  | Room | A | A | C | AB | AB | C | A | A | B |
| Chloric Acid |  | Room |  |  | A |  |  | C |  |  |  |
| Chlorosulfonic Acid | 10% |  | A | A | C | AB | AB | C | A |  |  |
| Chromic Acid | 5% | Room | C | A | A |  | AB | A | A | A |  |
| Chromic Acid, C.P. | 10% | Boiling | C | A | C | C | C | B | A | A |  |
| Chromic Acid | 50% | Boiling | C | B | C | C | C | C | A | B |  |
| Citric Acid | 5% Still | 150 0 | A | A | A | AB | AB | A | A | A | A |
| Citric Acid | 15% | Room | A | A | A | AB | AB | A | A | A | A |
| Citric Acid | 15% | Boiling | A | A | A |  | AB | A | A | A | A |
| Citric Acid | Concentrated | Boiling | A | A | A |  |  | B | A | A | AB |
| Fatty Acids |  |  | A | A | A | AB | AB |  | A |  |  |
| Formic Acid | 5% Still | Room to 150 0 | A | A | A | AB | AB | (A | A |  | A |
| Gallic Acid | 5% | Room to Boiling | A | A | A |  | AB | A |  |  |  |
| Hydrobromic Acid |  | Boiling | A | B | C | C | C | C | A |  |  |
| Hydrochloric Acid | 5% Unaerated | Room | B | A | C | AB |  | C | A | B | A |
| Hydrochloric Acid | 10% Unaerated | Room | A | A | C | B | C | C | A | B | A |
| Hydrochloric Acid | 20% Unaerated | Room | A | A | C |  |  | C | A | C | A |
| Hydrochloric Acid | All | 100 0 F | A | A | C |  |  | C | A | C | A |
| Hydrochloric Acid | All | 122 0 F | B | B | C |  |  | C | A | C | A |
| Hydrochloric Acid | All | 160 0 F | A | B | C |  |  | C | A | C | A |
| Hydrochloric Acid Fumes | Concentrated | 100 0 |  |  | C |  |  | C | A | C | C |
| Hydrocyanic Acid |  |  | A | A | A | AB |  | A | A |  |  |
| Hydrocyanic Acid | All | All | A | A | C | AB |  | C | C | C | C |
| Hydrofluoric Acid Vapors |  | 2120 | A | A | C | AB |  | C | C |  | C |
| Hydrofluosilicic Acid | 5% | 700 | A | A | A | AB |  | C | C | C |  |
| Hydrofluosilicic Acid Vapors |  | 212o |  |  | C | AB |  | C | C |  |  |
| Lactic Acid | 5% | Room | A | A | A | AB | AB | A | A | A | A |
| Lactic Acid | 5% | 1500 | A | A | A |  |  | A | A | A | A |
| Lactic Acid | 10% | 1500 to Boiling | A | A | A |  |  | B | A | A | AB |

| CORROSION DATA - ACIDS (continued) | Hastelloy "B" | Hastelloy "C" | Carpenter 20 | Monel | Inconel | Stainless Steel 316 | Tantalum | Titanium | Zirconium |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Media | Concentration | Temperature 0F |  |  |  |  |  |  |  |  |  |
| Malic Acid |  | Cold & Hot | A | A | A | AB | AB | A | A |  |  |
| Molybdic Acid | 5% | Room | A | A | A |  |  | A | A |  |  |
| Muriatic Acid |  | Room | A | A | C |  |  | C | A |  |  |
| Nitric Acid | 5% | Room | C | A | A | C | C | A | A | A | A |
| Nitric Acid | 20% | Room | C | A | A | C | C | A | A | A | A |
| Nitric Acid | 50% | Room | C | A | A | C | AB | A | A | A | A |
| Nitric Acid | 50% | Boiling | C | C | A | C | C | A | A | A | A |
| Nitric Acid | 65% | Boiling | C | C | A | C | C | B | A | A | A |
| Nitric Acid | 95% | Room | C | A | A |  |  |  | A | A | A |
| Nitric Acid | Concentrated | Room | C | A | A |  |  | A | A | A | A |
| Nitric Acid | Concentrated | Boiling | C | C | A |  |  | B | A | A | A |
| Nitric Acid | Fuming | Room | C | A | A |  |  | A |  | A | A |
| Nitrous Acid | 5% | Room |  |  | A |  |  | A | A |  |  |
| Oleic Acid |  | Room | A | A | A | AB | AB | A | A |  |  |
| Oleic Acid | 5% | Cold & Hot | A | A | A | AB |  | A | A | C |  |
| Oleic Acid | 10% | Room | A | A | A | AB |  | A | A | A | AB |
| Oleic Acid | 10% | Boiling | B | A | A | AB |  | C | A | C | AB |
| Phosphoric Acid | 1% | Room | A | A | A | AB |  | (A | A | A | A |
| Phosphoric Acid | 5% | Room | A | A | A | AB |  | A | A | A | A |
| Phosphoric Acid | 10% Still | Room | A | A | A | AB | AB | A | A | A | A |
| Phosphoric Acid | 10% Agitated | Room | A | A | A | AB |  | A | A | A | A |
| Phosphoric Acid | 10% Aerated | Room | A | A | A |  |  | A | A | A | A |
| Picric Acid | Concentrated | Room | A | A | A | AB |  | A |  |  |  |
| Pyrogallic Acid |  |  | A | A | A |  |  | A |  |  |  |
| Salicylic Acid |  |  | A | A | A | AB |  |  | A |  |  |
| Stearic Acid | Concentrated | 200 0 | A | A | A | AB | AB | A | A | A |  |
| Succinic Acid |  | Molten | B | B |  |  | AB |  |  |  |  |
| Sulfuric Acid | 5% | Room | A | A | A | AB | AB | B | A | B | A |
| Sulfuric Acid | 5% | Boiling | A | B | A | C | C | C | A | C | A |
| Sulfuric Acid | 10% | Room | A | A | A | AB |  | B | A | B | A |
| Sulfuric Acid | 10% | Boiling | A | B | B | C | C | C | A | C | A |
| Sulfuric Acid | 50% | Room | A | A | A | AB |  | C | A | B | A |
| Sulfuric Acid | 50% | Boiling | A | C | BC | C | C | C | A | C | A |
| Sulfuric Acid | Concentrated | Room | A | A | A | AB |  | A | A | C | C |
| Sulfuric Acid | Concentrated | Boiling | C | C | C | C | C | C | C | C | C |
| Sulfuric Acid | Concentrated | 300 0 | C | C | BC | C | C | C | C | C | C |
| Sulfuric Acid | Fuming | Room | A | B | A | C | C | B | C |  |  |
| Sulfuric Anhydride | Dry | Room | A | A |  | C | C |  | C |  |  |
| Sulfurous Acid | Saturated | 375 0 | C | A | A | C | C | B | A |  | B |
| Sulfurous Spray |  | Room | C | A | A | C | C | C | A |  |  |
| Tannic Acid | 10% | Room | A | A | A | AB | AB | A | A | A | A |
| Tannic Acid |  | 150 0 | A | A | A |  |  | A | A | A | A |
| Tartaric Acid | 10% | Room | A | A | A | AB |  | A | A | A | B |
| Tartaric Acid |  | 150 0 | A | A | A |  |  | A | A | A |  |
| Trichloro acetic Acid |  | Room |  |  |  |  |  | C |  | C |  |
| Uric Acid | Concentrated |  | A | A | A |  | AB | A |  |  |  |

| CORROSION DATA - MISCELLANEOUS | Hastelloy "B" | Hastelloy "C" | Carpenter 20 | Monel | Inconel | Stainless Steel 316 | Tantalum | Titanium | Zirconium |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Media | Concentration | Temperature 0F |  |  |  |  |  |  |  |  |  |
| Acetone |  | Boiling | A | A | A | A | A | A | A |  |  |
| Alcohol - Methyl, Propyl Butyl, Ethyl |  | Room | A | A | A | A | A | A | A | A | A |
| Alkaform |  |  | A | A |  |  |  | A |  |  |  |
| Aluminium |  | Molten | C | C |  | C | C | C | C |  |  |
| Aniline | Conc. | Room | A | A | A |  |  | A | A |  |  |
| Baking Oven Gases |  |  | A | A |  |  | AB | A | A |  |  |
| Beer |  |  | A | A | A | AB |  | A | A |  |  |
| Benzene |  | Room | A | A | A | AB | AB | A | A | A |  |
| Benzol |  | Hot | A | A | A | AB | AB | A | A |  |  |
| Bleaching Powder | Solution | Hot | C | A | AB | C | C | AB | C |  |  |
| Blood (Meat Juices) |  | Cold | A | A | A | A | A | A | A |  |  |
| Borax |  | Fused | A | A |  | AB |  | A | C |  |  |
| Bromine | Dry |  | C | A | A | A | A | C | A |  |  |
| Bromine Water |  | Room | C | A | AB | C | C | C | A |  | C |
| Buttermilk |  | Room | A | A |  |  | A | A | A |  |  |
| Camphor |  |  | A | A | A |  |  | A | A |  |  |
| Carbonated Beverages |  |  | A | A | A | AB | AB | A | A |  |  |
| Carbon Monoxide Gas |  | 900 0 | A | A | A | A | A | A | C |  |  |
| Cadmium |  | Molten | C | C |  | C | C | C | A |  |  |
| Caustic Lime |  |  | A | A |  | A | A | A | A |  |  |
| Caustic Soda |  |  | A | A | A | A | A | A | C |  |  |
| Chlorinated Water | Saturated | Room | C | A | A | C | C | (B | A | A | C |
| Chlorine Gas Dry |  | Room | A | A | A | A | A | C | A | C | B |
| Chlorine Gas Moist |  | Room | C | A | C |  |  | C | A | A | C |
| Chlorine Gas Moist |  | 212 0 | C | C | C | C | C | C | A | A | C |
| Chloroform |  | Room | A | A | A | A | A | A | A | A | A |
| Chromium Plating Bath |  | Room |  |  | AB | C | C | AB | A |  |  |
| Cider |  | Room | A | A | A | A | A | A | A |  |  |
| Coffee |  | Boiling | A | A | A | AB |  | A | A |  |  |
| Copal Varnish |  |  | A | A | A | AB |  | A | A |  |  |
| Cream of Tartar |  |  |  |  | A |  |  | A | A |  |  |
| Creosote (Coal Tar) |  | Hot |  |  | A |  | A | A | A |  |  |
| Crude Oil |  |  | A | A | A | AB |  | (A | A |  |  |
| Developing Solutions |  | Room | A | A | A |  | A | A | A |  |  |
| Distillery Wort |  |  |  |  |  |  |  | A | A |  |  |
| Dyewood, Liquor |  | Room |  |  |  |  |  | A | A |  |  |
| Ether |  | Room | A | A | A | AB | AB | A | A |  |  |
| Flue Gases |  |  | B | A | AB |  | AB | AB | A |  |  |
| Fluorine |  | Room |  |  | BC | A | A | C | C |  |  |
| Food Pastes |  |  | A | A |  | AB | AB | A | A |  |  |
| Formaldehyde |  | Room | A | A | A | B | AB | (A | A | A |  |
| Fuel Oil |  | Hot | A | A | A | AB | AB | A | A |  |  |
| Fuel Oil (Containing H2SO4) | Hot | A | A | A | B |  | B | A |  |  |

| CORROSION DATA - MISCELLANEOUS (continued) | Hastelloy "B" | Hastelloy "C" | Carpenter 20 | Monel | Inconel | Stainless Steel 316 | Tantalum | Titanium | Zirconium |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Media | Concentration | Temperature 0F |  |  |  |  |  |  |  |  |  |
| Fruit Juices |  | Room | A | A | A | AB | AB | A | A |  |  |
| Furfural |  |  | A | A | A | AB |  | A | A |  | A |
| Gasoline |  |  | A | A | A | AB | AB | A | A |  |  |
| Glauber's Salt | Solution | Hot | A | A | A | AB |  | A | A |  |  |
| Glue - Dry |  | Room | A | A | A |  |  | A | A |  |  |
| Glue - Solution Acid |  | Hot | A | A | A |  | AB | A | A |  |  |
| Glycerine |  | Room | A | A | A | AB |  | A | A |  |  |
| Gypsum |  |  |  |  | A |  |  | A | A |  |  |
| Hydrocarbons |  |  | A | A | A | AB | AB |  | A |  |  |
| Ink |  |  | A | A | A | AB | AB | A | A |  |  |
| Iodine |  |  | C | A | C | C | B | C | A |  |  |
| Iodoform |  |  |  |  |  |  |  | A | A |  |  |
| Kerosene |  | Room | A | A | A | AB |  | A | A |  |  |
| Ketchup |  | Room | A | A | A | AB |  | A | A |  |  |
| Lard |  | Room | A | A | A |  |  | A | A |  |  |
| Lead |  | Molten | A | A |  | C | C | C | A |  |  |
| Linseed Oil |  |  | A | A | A | AB | A | A | A |  |  |
| Lye (Caustic) | 34% | 230 0 | A | A | A | A | A | A | C |  |  |
| Lysol |  | 212 0 | A | A | A | A | A | (A | A |  |  |
| Mayonnaise |  | Cold & Hot | A | A |  | AB | AB | A | A |  |  |
| Meats (Unsalted) |  | Room | A | A | A |  |  | A | A |  |  |
| Mash |  | Hot | A | A |  |  |  | A | A |  |  |
| Mercury |  |  | A | A | A | AB | A | A | A |  |  |
| Milk - Fresh or Sour |  | Hot or Cold | A | A |  |  | A | A | A |  |  |
| Mine Water - Acid |  |  | A | A | A | C | C | (A | A |  |  |
| Molasses |  |  | A | A |  | A | A | A | A |  |  |
| Mustard |  | Room | A | A |  | AB |  | (A | A |  |  |
| Naptha |  |  | A | A | A | AB | AB | A | A |  |  |
| Nitre Cake |  | Fused |  |  |  |  |  | A | C |  |  |
| Oils - Crude |  | Hot & Cold | A | A | A | AB |  | (A | A |  |  |
| Oils – Mineral - Vegetable |  | Hot & Cold | A | A | A | AB | AB | A | A |  |  |
| Paraffin |  | Molten | A | A | A | AB |  | A | A |  |  |
| Paragoric Compound |  |  | A | A |  |  |  | A | A |  |  |
| Petroleum Ether |  |  | A | A | A |  |  | A | A |  |  |
| Phenol |  |  | A | A | A | A | A | A | A | A |  |
| Petrolic Resins |  |  | A | A | A |  |  | A | A |  |  |
| Pine Tar Oil |  |  | A | A | A | AB |  | A | A |  |  |
| Potash | Solution | Hot | A | A | A | A | A | A | C |  |  |
| Resin |  | Molten | A | A | A |  | AB | A | A |  |  |
| Sal Ammoniac | 20% | Boiling | A | A | A | AB |  | B | A |  |  |
| Salt | Saturated | Room | A | A | (A | A | A | (A | A | A | A |
| Salt Brine | Saturated | Hot | A | A | (A | AB | AB | (A | A | A |  |
| Sea Water |  |  | A | A | A | AB | AB | (A | A | A | A |

| CORROSION DATA - MISCELLANEOUS (continued) | Hastelloy "B" | Hastelloy "C" | Carpenter 20 | Monel | Inconel | Stainless Steel 316 | Tantalum | Titanium | Zirconium |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Media | Concentration | Temperature 0F |  |  |  |  |  |  |  |  |  |
| Sewage |  |  |  |  |  |  |  | (A | A |  |  |
| Soaps |  | Room | A | A | A | AB |  | A | A |  |  |
| Soy Bean Oil |  |  | A | A | A | AB |  | A | A |  |  |
| Soda Pulp |  |  | A | A |  | A | A |  |  |  |  |
| Starch | Solution |  |  |  |  |  |  | A | A |  |  |
| Steam |  |  |  |  | A | A | A | A | A |  |  |
| Sugar Juice |  |  | A | A | A | A | A | A | A |  |  |
| Sulfur -Dry |  | Molten | A | A | A | C | C | A | A |  |  |
| Sulfur - Wet |  |  |  |  | A | C | C | (A | A |  |  |
| Tin |  | Molten | A | A |  | C | C | C | A |  |  |
| Tomato Juice |  | Room | A | A | A | AB | AB | (A | A |  |  |
| Turpentine Oil |  |  | A | A | A | AB |  | A | A |  |  |
| Tung Oil |  |  | A | A | A |  | AB | A | A |  |  |
| Varnish |  |  | A | A |  | AB | AB | A | A |  |  |
| Vegetable Juices |  |  | A | A | A | AB | AB | A | A |  |  |
| Vinegar – Still |  | Room | A | A | A | AB | AB | A | A |  | A |
| Vinegar – Agitated |  | Room | A | A | A |  | AB | A | A |  |  |
| Vinegar – Aerated |  | Room | A | A | A |  | AB | A | A |  |  |
| Vinegar – Fumes |  |  | A | A | A |  | AB | (A | A |  |  |
| Vinegar and Salt |  |  | A | A | A |  | AB |  | A |  |  |
| Water |  |  | A | A | A | A | A | A | A | A | A |
| Water – Hot |  |  | A | A | A | A | A | A | A | A | A |
| Water – Salt |  |  | A | A | A | AB | AB | (A | A | A | A |
| Water – Sea |  |  | A | A | A | AB | AB | (A | A | A | A |
| Whiskey |  |  |  |  |  | A | A | A | A |  |  |
| Zinc |  | Molten | C | C |  | C | C | C | A |  |  |